## Slide 1
Alyza Khan, Dr. Greg Ogden
Department of Chemical & Environmental Engineering
University of Arizona
Design and Testing of Polymer Electrolyte Membrane (PEM) Hydrolysis System for Producing Hydrogen and Oxygen Propellants for CubeSat Applications

## Slide 2: Agenda
Motivation
  Where we fit in
Objective
Challenges
Method
Analysis/Results
Discussion
Takeaway

## Slide 3: Big Picture: Green Propulsion System Development
Electrolyzer Experiments
(This Talk)
Combustion Experiments
Pressurization Experiments

## Slide 4: Objectives
  Develop 1U CubeSat Propulsion System using commercial Polymer Electrolyte Membrane (PEM) Electrolyzers
    Water propellant storage medium
    Electrolyzers produce hydrogen and oxygen for propulsion
Double Electrolyzer
$100
Single Electrolyzer
$80
Single Rebuildable Electrolyzer
$200

## Slide 5: Challenges
Building the entire experimental apparatus in our lab
  Pressurizing the system with Hydrogen & Oxygen instead of Nitrogen
  Leak testing and calculating impact on data accuracy
  Back pressure regulator operation
  Testing different Educational Electrolyzers
  Making and accounting for modifications to various Units
  Coordinating support for testing

## Slide 6: Experimental Plan
Parameters Measured: Hydrogen & Oxygen Flowrates and Current

## Slide 7: Experimental Apparatus
Water Pump
Hydrogen Cylinder + Pressure gauge
Hydrogen Flowmeter
Hydrogen BPR
Oxygen Cylinder + Pressure gauge
Power Supply

## Slide 8: HTec Double Electrolyzer Tested at 3.5V

## Slide 9: HTec Single Rebuildable Electrolyzer Tested at 2V

## Slide 10: HTec Single Electrolyzer: Tested at 2V

## Slide 11: HTec Double Performance @ 3.5V
Chart: Pressure, psig
| 7 | 15 | 29 | 46 | 59
H2 | 8.7387 | 8.2252 | 8.8883 | 7.1353 | 6.7647
O2 | 3.7355 | 3.3952 | 3.7638 | 2.8027 | 2.8521
Current | 0.53571 | 0.49286 | 0.475 | 0.41333 | 0.41333

## Slide 12: HTec Rebuildable Performance @ 2V
Chart: Pressure, psig
| 7 | 15 | 29 | 44 | 59 | 73
H2 | 8.3333 | 8.1032 | 8.1258 | 7.8383 | 6.9642 | 6.5594
O2 | 3.2351 | 3.234 | 3.765 | 2.8452 | 3.7939 | 2.4771
Current | 1.0467 | 1.0183 | 1.0217 | 0.97833 | 0.955 | 0.91

## Slide 13: HTec Single Performance @ 2V
Chart: Pressure, psig
| 6 | 15
H2 | 4.9988 | 5.1834
O2 | 2.2667 | 2.3119
Current | 0.42333 | 0.31833

## Slide 14: Data Summary
HTec Double
  Operated at Pressures up to 4 atm
  Current and Pressure are inversely proportional
  Flowrates and Current are directly proportional
HTec Rebuildable
  Operated at Pressures up to 5 atm
  Current and Pressure are inversely proportional
  Flowrates and Current are directly proportional
HTec Single
  Only worked well under ambient conditions
    Failed at pressures above 20psig

## Slide 15: Conclusion & Discussion
Tested 3 commercial/educational electrolyzer units
  2 worked, 1 failed
Increasing Pressure reduces Current and Flow
  Large variability in H2 flow rates
Feasibility of using Educational Units determined
Next steps:
  Correlate gas production rates to surface area
  Resolve water pressurization issues
  Test other units, alternate membranes

## Slide 16: Questions?
Thank you