## Slide 1
Fast Transit Missions with Extreme Solar Sailing
Artur Davoyan
University of California,
Los Angeles

## Slide 2
9 missions
4 missions
1 mission
1 mission
1 mission
Deep Space Exploration Today
2 missions
60 years of space exploration
2 missions

## Slide 3
Search for life
Need to scale exploration
Travel takes many years (>7 years to Saturn)
Missions require decades long costly (~$1B) development
Need For Breakthrough Science
Outer planets & moons
Our star
Interstellar medium & beyond
Understanding our Sun
Need inner corona observations
4D mapping of the corona
Going to far reaches
Only two probes have reached the interstellar medium
Planet X?
Oort cloud
Solar gravity lens

## Slide 4
State Of The Art: Outer Space
Voyager 1 (1977) is the fastest spacecraft ever built.
Travelling at a record 17km/s it took 35 years to reach interstellar medium at 120 AU (the first spacecraft to reach this milestone).
Most distant spacecraft as of today (155 AU after 45 years of travel)
Image credit: NASA

## Slide 5
Limitations Of Propulsion
Limited by the rocket equation
Need to carry fuel and “throw” it away to propel

## Slide 6
Image credit: the Planetary Society
Solar sails

## Slide 7
Solar sail missions flown and planned
NanoSail-D (2010)
NASA
Earth orbit
Deployment Test
3U CubeSat
10 m2
IKAROS (2010)
JAXA
Interplanetary
mission
315 kg, SmallSat
196 m2
LightSail-1 (2015)
The Planetary Society
Earth Orbit
Deployment Test
3U CubeSat
32 m2
7
NEA Scout (2021)
NASA
Interplanetary mission
6U CubeSat
86 m2
8

## Slide 9
Goal: fast
Sail area: ~100m x 100m
Payload mass: 10-20 kg
Overall S/C mass: ~50 kg
Cost: <$100M
How fast can we go?
>20 AU/yr (up-to 60 AU/yr)
<10 R☼

## Slide 10
Where is the limit?
Parameter | Range
Spacecraft bus mass (excluding sail systems) | 10-20 kg
Sail area | 10,000 m2 – 25,000 m2
Perihelion pass | 3-5R☼
Sail material density | <1 g/m2
Sail material reflectivity | > 0.7
Parameters needed for 60 AU/yr

## Slide 11
Trajectory & mission profile
C3=0
Start with MEO and “spiral out”
5R☼ perihelion
100% reflectivity
A.R. Davoyan et al., Optica 8, 722 (2021)
7 days between entering and leaving Mercury orbit
150 days to reach perihelion

## Slide 12
Getting Close To The Sun
Outstanding mission challenges
Harsh environment
Need for new materials
Large lightweight architectures
Spacecraft controls & navigation
Power and communications

## Slide 13
Heavy heat shield
Radiation, plasma, particles
Grand challenge
Parker solar probe
(9 R☼)

## Slide 14
Credit: NASA
Current sail material technology

## Slide 15
Limitations of current materials
Al (50 - 100 nm)
Organic film (few )
Sunlight
Heat rejection
*10% - Al absorbance
*0.04 – Al emissivity
Kapton
Mylar, CP1
Al

## Slide 16
Chart: Closest approach (solar radii)
| 2
Al2O3 | 2070
cBN | 3000
hBN | 3000
HfO2 | 2774
Si3N4 | 1900
SiC | 2830
SiO2 | 1900
TiN | 3290
TiO2 | 1843
graphene | 3600
HfN | 3305
NbC | 3490
Extreme sail materials
Refractory metals: Titanium nitride, tungsten
Transparent ceramics

## Slide 17
Two types of sail materials
TiN sails
TiN
High temperature inorganic film
100nm
500nm-1000nm
Bragg reflectors
Photonic crystals
SiN metamaterial sails
>70% reflection, <0.7 g/m2, survive at <5R☼
High T
Easy to make
Lower T
Harder to make

## Slide 18
TiN sails
TiN
High temperature inorganic film
100nm
500nm-1000nm
High T
Easy to make
Estimated density: <1.5 g/m2
Tested at ~500C (no degradation found)
High melting point (3200 degree C) – can survive around 2.5 solar radii
Density: 5.4 g/cm3
Absorbs 40% of sunlight

## Slide 19
Ultrathin films
~100 nm thick free standing Al/CNT films
Coated with CNTs on the backside
front
back
Wavelength (nm)
Reflectance
Estimated density: <1.5 g/m2
Tested at ~500C (no degradation found)

## Slide 20
Toward TiN sail materials
LEO environmental testing via MISSE mission
(launched Aug 29th, 2021)
Thanks to Miria Finckenor (NASA MSFC)

## Slide 21: Sail craft architecture
~10kg spacecraft bus,
~0.7g/m2 sail material areal density,
50-70g/m boom density
150m by 150m sail
(A/m = 554 m2/kg) & v>50 AU/yr
 | Bus | Sail support/booms | Sail material | Total
Mass (kg) | 10 | 14.8 | 15.75 | 40.55
Fraction (%) | 25% | 36% | 39% | 100%
Payload protection
Control authority
Power & mass budget
<50 W (RTG)
Optical comms
Total bus mass ~10 kg
H+ energy ~1keV
Solar wind
300km/s
100nm
200nm
Sputtered atoms
Interaction with solar plasma
All aspects of the mission are feasible and doable

## Slide 22: Roadmap

## Slide 23
Vision: Sun as a Launch Pad
Oort cloud
Kuiper belt
Goals:
low cost (~$10M)
short lead time
missions to arbitrary destinations (e.g., high inclination)
fast (50-60 AU/year)

## Slide 24: Team and Acknowledgements
PI: Artur Davoyan
Co-Pis: Henry Helvajian, Les Johnson, Marco Velli
Collaborators: S. Turyshev (JPL), D. Garber (NXtrac), L. Friedman (Planetary Society), P. Hon (Northrop Grumman), J. Carr (MSFC), M. Nehls (MSFC), M. Finckenor (MSFC)
UCLA student team: H.T. Tung, H. Ling, P. Krings, J. Digani, S. Huang, A. Dunn, S. Martinez, R. Rio