## Slide 1: Ultrathin carbon nanotube freestanding thin films with specular reflective coatings for small satellites
Ho-Ting Tung, Evy Haynes, Artur R. Davoyan
Concept art of The Planetary Society's LightSail 2 spacecraft
Mechanical and Aerospace Engineering
UCLA

## Slide 2: Thin film material for small sat
Advantages of thin film materials on spacecraft:
Lightweight
Flexible
Deployable
Possible applications
Thermal control (radiators)
Plasma/radiation protection
Radiation pressure attitude control systems…
Image credit: NASA/JPL-Caltech

## Slide 3: Thin film material in space
Large Deployable Antenna
Image credit: ESA
Deployable membrane-like mirror
Image Credit: M. Ulmer, Northwestern University
Image credit: NASA
Solar sailing
Explore new thin film materials for new degrees of control
Density
Operation temperature
Optical property

## Slide 4: Carbon nanotube thin film
Lightweight (~1g/m2).
High thermal conductivity
Heat resistivity (melting point ~3500 °C)
Plasma resilience
Good mechanical properties
Large scale fabrication
~1m CNT thin film
CNT sample
NEA scout
Image credit: NASA
2.5 m Mylar
Aluminum
Melting point
~250°C

## Slide 5: Exploring optical properties
Rough surface morphology,
Lack of control in optical properties
-> New fabrication approach needed
CNT thin film
Reflective layer
Al directly deposited on CNT film
Rough surface

## Slide 6: Functionality tests
Directly deposition on CNT film: rough
New fab approach:
Optically smooth
Survives 450°C (Comparing to Mylar films melting point ~250°C)
Specular reflective front side
Rough
2cm
Back side
Back side with CNT

## Slide 7: Other surface coatings
We achieved controllable optical properties on other surface coatings too!

## Slide 8: Case study on solar sailing
What is Solar Sailing?
In space propulsion method that utilize radiation pressure from the sun to propel the spacecraft.
Thrust
Reflection
Solar sail
Past Missions
Lightsail 2 (2019)
CubeSat missions
Near Earth missions
Image credit: NASA
Nanosail-D (2010)
Image credit: NASA
Notes: Polyimide film
Degrade at less than 450 deg C

## Slide 9: Thin film materials in solar sailing
Low density: lightweight spacecraft to enable high velocity change
Controllable optical properties: Specular reflective to generate thrust
High operation temperature:
  Better thermal management
  Get close to the sun
  Intense solar radiation
  High thrust!
Notes: Polyimide film
Degrade at less than 450 deg C

## Slide 10: Thin film materials enables better science!
Image credit: Princeton Satellite Systems
Solar polar imager trajectory
~0.5AU
With advanced thin film materials:
<0.2AU
Image credit: Artur Davoyan
Explore science near the sun
More efficient solar sailing…
Tested under temperature 200 degree higher than Mylar melting point

## Slide 11: Conclusion
Thin film materials enables small satellite compatible components and instruments.
New thin film materials are explored for degrees of control in density, optical properties, and operational temperature.
Acknowledgements
Artur Davoyan
Evy Haynes